Effect of carbon doping on Ge(001)/Mn5Ge3 thin films grown by magnetron sputtering technique

A. Alvídrez-Lechuga1, R. López-Antón2, L. E. Fuentes-Cobas1, J. T. Holguín-Momaca1, C. Santillán-Rodríguez1, S. F. Olive-Méndez1

1Centro de Investigación en Materiales Avanzados, S.C. (CIMAV), Miguel de Cervantes 120, C.P. 31136, Chihuahua, Chih, Mexico.

2Instituto Regional de Investigación Científica Aplicada (IRICA), Departamento de Física Aplicada, Universidad de Castilla-La Mancha, 13071 Ciudad Real, Spain.

Email: adriana.alvidrez@cimav.edu.mx

In the last decade Mn5Ge3 thin films have attracted much attention due to their magnetic and structural properties, well-suited for spintronics [1]. One of the major challenges on the design of spintronic devices, as the spin-FET, is the achievement of spin injection into a semiconductor at room temperature (RT) [2]. A heterostructure that provides a better approach for this purpouse is a ferromagnetic (FM)/semiconductor multilayer with a Schottky barrier at the interface. Mn5Ge3 compound has become an important material for its FM ordering with a TC = 296 K, that increases with carbon doping. The hexagonal crystal structure allows the growth on Ge(111) substrates within a lattice mismatch of 3.7%. However, Ge(111) is not compatible with the Si(001) technology [3]. Ge(001)/Mn5Ge3 heterostructures offer the possibility of spin injection into IV-group semiconductors.

This work shows the synthesis and characterization of Ge(001)/Mn5Ge3 thin films elaborated by magnetron sputtering using the solid phase epitaxy (SPE) method at 250 °C. Figure 1(a) shows the bi-dimensional grazing incidence x-ray diffraction (2D-GIXRD) patterns collected at beamline 7.1 MCX (Elettra Synchrotron) for a sample without carbon and (b) a sample doped with carbon. Both patterns show discontinuous Debye rings that are associated to the texture. Figure 1(c) shows a representative high resolution transmission electron micrograph related to the epitaxial growth of a sample grown by co-deposition of Mn and C, followed by a co-deposition of Mn, Ge and C.

Figure 1. 2D-GIXRD comparison between a sample (a) without carbon and (b) a sample doped with carbon. (c) A sample grown by co-deposition of Mn and C, followed by co-deposition of Mn, Ge and C.

References

[1] A. Alvídrez-Lechuga, R. López-Antón, J. T. Holguín-Momaca et al 2016 Thin Solid Films 616, 111–115.

[2] A. Alvídrez-Lechuga, J. T. Holguín-Momaca, C. R. Santillán-Rodríguez et al 2017 Superficies y Vacío 30(4), 61-64.

[3] A. Alvídrez-Lechuga, R. López-Antón, L. E. Fuentes-Cobas et al 2018 J. Alloys Compd. 762, 363-369.